Title: Auger Electron Spectroscopy

Submitted By

- Ravish Kumar 		(05-07-00-10-41-12-1-09887)

- Aasik V			(05-07-00-10-41-12-1-09885)

- Mohit Mathur		(05-07-00-36-41-12-1-10006)

- Ravi Jai Prakash		(05-07-00-36-41-12-1-10004)

Auger Electron Spectroscopy:

“Three Electron process”*

“Leaves doubly ionized atoms”

Process Step 1:

Atomic ionization (photo emission process): Initial core hole can be generated by exposing the sample to a beam of high energy electrons (typically in the range of 2-10KeV)

Process Step 2:

Relaxation & auger emission: Electron in highly excited state will relax back to by one of the two routes:

- Auger transmission (Non-Radiative transition: low energy transition) < 500eV

- X-ray fluorescence (Radiative transition: high energy transition)  > 2000Ev

Kinetic Energy of Auger Electron

KE ~ EA - EB - EC

EA - EB = emitted energy of relaxed electron,

EC = Energy needed to overcome the binding energy of auger electron

Note:  Kinetic energy of auger electron is not α to the primary beam energy (different from XPS)

Auger transition Notation:

K L2,3 L2,3

K - Initial core hole

L - Origin of relaxing electron

L - Source of auger electron

- Four main auger series are: KLL, LMM, MNN, and NOO

- Auger transition can take place in all atoms except Helium & Hydrogen (?)*

- Auger spectra contains closely spaced groups of multiple peaks

- Auger Spectra are often reported in differentiated from dN(E)/dE – for better sensitivity

- Qualitative analysis :  surface composition analysis

- Interpretation of AES spectra is more difficult than XPS.

AES Electron Kinetic Energy Vs Atomic number